# Water Contamination Research

Collected Notes on Toxics Leaching from Plastic, Metal and Cementations Containers, Bacterial Regrowth, and Disinfection Byproducts

May 2005

This document is designed to be viewed in OUTLINE mode in Microsoft Word.

These are the raw research notes for Water Storage by Oasis Design.

There is no analysis or synthesis here. The health effects depend on the:

- Material

- Additives, mold-release agents, coatings, etc.

- Contact time

- Contact area

- Temperature

- Age of the material (some become less noxious with time, some more)

- Exposure to sunlight

- Susceptibility of the individual

To the extent we were able to make any sense of the information below, our analysis can be found in our water storage book:

http://www.oasisdesign.net/water/storage/

Much of this material is copyrighted by others and is reproduced here under the “fair use” doctrine. The source for the material is given at the start of each section.

# Water Quality Standards

## National Primary and Secondary Drinking Water Regulations

http://www.epa.gov/safewater/mcl.html

http://www.ehso.com/ehshome/DrWater/drinkingwaterstds.htm

National Primary Drinking Water Regulations (NPDWRs or primary standards) are legally enforceable standards that apply to public water systems. Primary standards protect drinking water quality by limiting the levels of specific contaminants that can adversely affect public health and are known or anticipated to occur in public water systems. Table 1 divides these contaminants into Inorganic Chemicals, Organic Chemicals, Radionuclides, and Microorganisms. See Setting Standards for Safe Drinking Water to learn about EPA's standard-setting process. Follow these links to download copies of National Primary Drinking Water Regulations and National Secondary Drinking Water Regulations.

## National Sanitation Foundation. 2001. NSF Standard 61 Drinking Water System Components—

http://www.nsf.org/Certified/PwsComponents/

Searchable database of certified components

# Leaching from metals

## Lead

http://www.denverwater.org/waterquality/pbwater.html - Where

Brass faucets can legally contain as much as eight percent lead by weight. Solders and flux are considered lead free when they contain not more than .2 percent lead. Before 1987, solder normally contained about 50 percent lead.

Always use cold water for food and beverage preparation. Hot tap water can leach higher amounts of lead or other metals from plumbing or the hot water tank. If you're concerned about elevated lead levels in your water, run the tap until the water becomes colder before using it. Remember to catch the flushed water for plants or other household use.

## Aluminum

### Aluminum Toxicity:  Issues and Insights

http://www.bayeralbumin.com/web_docs/WP_Aluminum Toxicity.pdf

“People are continuously exposed to Al by ingesting water, food, and dust particles. 2 Estimates suggest that adults consume approximately 3 to 5 mg of Al in their daily diet. Healthy individuals can easily handle normal Al intake, since absorption in the gastrointestinal (GI) tract is low. 4 The GI tract provides efficient protection against Al absorption, and it is estimated that less than 1% of ingested Al is absorbed by the body. 5 In fact, healthy individuals have very low levels of Al because the GI tract, skin, and lungs are effective barriers to Al absorption, and the kidneys efficiently eliminate absorbed Al by excretion.“

People who are at risk from aluminum poisoning:

Dialysis patients and others with impaired renal function

Newborns and premature infants

The elderly

Patients receiving TPN

Burn patients

Effects of aluminum toxicity:

Associated:

Dementia

Encephalopathy

Learning deficits

Possibly associated:

ALS

Parkinson’s disease

Alzheimer’s disease

### Report of the New South Wales Chief Health Officer, 1997

http://www.health.nsw.gov.au/public-health/chorep97/env_watalum.htm

Drinking water probably contributes less than 5 per cent of the total human intake of aluminium.  Although some studies have suggested a tentative link between aluminium and Alzheimer’s disease and  dementia, the evidence as a whole does not support a causal association. Accordingly, there is no  health-based guideline for aluminium in water.

## Copper

acidic water can deteriorate copper pipes.

http://www.boston.com/globe/search/stories/health/how_and_why/041596.htm

## A Comparison of Metal Leachate Rate and Zebra Mussel Control Efficacy for Coatings and Materials Timothy D. Race and Mark A. Kelly

sgnis.org/publicat/proceed/1994/319.pdf

ABSTRACT: Laboratory immersed test coupons of conventional antifouling coatings, metal pigmented coatings, thermal-sprayed metallic coatings, and metal substrates were evaluated for metal ion release rates over a 2-year period. Identical test coupons were evaluated for fouling over a 15-month period at Black Rock Lock,Buffalo, NewYork. This paper compares the efficacy of these materials and their release rates as a function of time. Other antifouling products,  including capsaicin-based coatings and a biocide impregnated plastic,were evaluated at the field site. Control panels are heavily infested after 15-months while the majority of test materials continue to prevent zebra mussel  attachment.  Estimated minimum  effective  release  rates  for copper and zinc are determined.

Metal Substrates. Copper and brass sheet materials were completely effective against the zebra mussel over the 15-month test period. Aluminum-bronze had a low colonization rate. From Figure 6 the downward trend in copper leach rate is fairly evident for each of these materials. The final data point for brass is probably aberrant and thus copper leach rates for the 3 materials follow the trend; copper> aluminum-bronze > brass. Brass also has a fairly steady zinc release of about 2 ug/cm 2 /day, which probably reinforces the materials’ efficacy. The copper leach rate for these materials progressively decreases with time. A direct time dependent relationship between field and laboratory exposed materials may not exist. In other words, the leach rates after 15-months of field and laboratory exposure are probably not the same. However, the trends and relative leach rates are probably reliable. The leaching data would seem to suggest that aluminum-bronze and copper sheet materials will eventually have copper leach rates too low to be effective. The decrease in leach rates are probably caused by the accumulation of insoluble corrosion products on the surface of the test materials. If this is the case, then periodic rejuvenation of these surfaces by means of light abrasion would be possible.

Zinc Containing Coatings. The thermal-sprayed zinc coating, the wafer-borne inorganic zinc coating, and galvanizing all exhibited relatively low levels of mussel attachment at 15-months. Zinc leach rates were approximately 6,3, and 5 ug/cm 2 /day, respectively, at 600 days of laboratory exposure. The zinc materials serve a secondary function as corrosion protection on steel substrates. Even at modest levels of colonization, zinc coatings would offer a significant advantage in terms of cost and simplicity over the other antifoulants. Zinc coatings marketed for corrosion protection do not require registration under the Federal Insecticide, Fungicide, and Rodenticide Act.

## Fish tank zinc

http://www.zetatalk.com/nonproft/99001991.htm

The fish tanks were closed down in mid-January, as a yellow dye in the fish food had cumulated to the point of poisoning the catfish. This was the only additive, and turned the clear water a mustard yellow and create a yellow foam. This was one of the lessons learned - in a closed cycle, one must take great care what is added to the system. (2002 Note: it has been learned that the galvanized tanks, which leach zinc, highly toxic to fish, were probably the culprit. An epoxy paint is recommended to prevent this in the future.)

# Coatings

http://www.epa.gov/safewater/tcr/pdf/storage.pdf

tank Turnover –no stagnant water

2.1.4 Chemical Contaminants

Coating materials are used to prevent corrosion of steel storage tanks and to prevent moisture migration in concrete tanks. Through the 1970's, coatings used in finished water storage facilities were primarily selected because of their corrosion resistance and ease of application. This led to the use of industrial products like coal tars, greases, waxes and lead paints as interior tank coatings. These products offered exceptional corrosion performance but unknowingly contributed significant toxic chemicals to the drinking water. Grease coatings can differ greatly in their composition from vegetable to petroleum based substances and can provide a good food source for bacteria, resulting in reduced chlorine residuals and objectionable tastes and odors in the finished water (Kirmeyer et al. 1999).

An old grease coating on a storage tank interior in the state of Florida was suspected of causing water quality problems in the distribution system such as taste and odor, high chlorine requirements and a black slime at the customers tap. The Wisconsin Avenue 500,000 gallon elevated tank was originally coated with a petroleum grease coating when it was built in 1925.

In 1988, the storage facility was cleaned and the grease coating was reapplied. In 1993, a tank inspection revealed that the grease had sagged off the tank walls and deposited a thick accumulation of black loose ooze in the bottom bowl of the tank (6-8 inches deep). A thin film of grease continued to coat the upper shell surfaces. Although this material had performed well as a corrosion inhibitor, it was introducing debris into the distribution system as well as creating a possible food source and environment for bacteria. The City decided to completely remove the grease and reapply a polyamide epoxy system. This work was completed in 1996 (Kirmeyer et al. 1999). Since the tank was returned to service, water quality has markedly improved. The required chlorine dosage rate has decreased from 4.0-5.0 mg/L to 3.5 mg/L. The chlorine residual at the tank outlet has improved from <1.0 mg/L to 1.4 mg/L. No more “black slime” complaints have been received.

## Epoxy

There is evidence that epoxy coatings leach various organic additives into water.

“Permeation and leaching”

http://www.epa.gov/safewater/tcr/pdf/permleach.pdf

The rate of leaching of organic additives was found to decrease exponentially with time. Therefore, it is recommended that newly lined pipes be pre-soaked prior to release to service. Normal hydrostatic testing and disinfection activities will help remediate leaching.  Extending the curing process will also help improve the stability of epoxy linings

# Leaching from plastics

## Potential water quality deterioration of drinking water  caused by leakage of organic compounds from  materials in contact with the water

Plastics keyProceedings, 20 th NoDig conference, Copenhagen May 28-31 2002.

Lars J. Hem, Aquateam AS, P O Box 6875 Rodeløkka, 0504 Oslo, Norway, E-mail lars.hem@aquateam.no  and Ingun Skjevrak,  Regional Food Control Authority, Stavanger, Norway   E-mail: skjevrak@nmt-mrog.rl.no      ABSTRACT    Organic materials have been used in drinking water pipes and storage tanks for several years. During the  last decade plastic materials are used for bottles and containers for water. Leaching of organic matter from  the materials to the drinking water is proven. Water in contact with plastic pipes, surface coatings or other  materials can be affected by migration of components that make the water quality unacceptable with respect  to aesthetic effects or health.      Leaching of - volatile organic compounds may cause unwanted taste and odour in - water, and possible  health risk. Organic compounds such as xylene, styrene, phenols and ethyl benzene have been identified.  Compounds leaching from epoxy and polyethylene appear to give unwanted taste and smell to the water.    Microbiological growth in the drinking water distribution system may cause deterioration of the water quality,  due to increased turbidity, heterotrophic bacteria, and even pathogens. Leakage of biodegradable organic  matter from materials used in the distribution system may promote microbiological growth. There are  variations in microbiological growth between various materials. In particular, the change from copper to  synthetic materials for in-house installations may be a reason for increased microbiological growth.

RELEVANT PIPE MATERIALS    Plastic materials used for service pipes may be made from PVC (polyvinyl chloride), HDPE (high density  polyethylene) or GRP (glass fibre reinforced polyester). In-house plastic plumbing materials will consist of  PVC or PEX (cross-bound PE).    Epoxy lining can be used on concrete and on stainless steel in pipes and basins.    Additionally, lubricants may be used for fitting pipes together, as well as in the production of, for instance,  stainless steel pipes.

Several complaints on drinking water quality in Norway or on offshore installations are related to volatile organic matter (VOC) leaching from epoxy lining or paint. Typical VOCs from epoxy are alkyl benzenes and alkoxy compounds -. In particular leaching of hydrocarbons from in-situ epoxy coated storage tanks offshore and on ships seems to be a problem, with a solvent (xylene/ethylbenzene) content of up to 60-70 µg/l being measured. C3- and C4 cyclohexanes and other alicyclic hydrocarbons have also been identified as taste and odour compounds leaching from surface coatings. In a treated water basin for municipal water supply, organosulphide compounds were identified as the source for taste and odour, and the most likely source of the sulphides produced was microbiological activity due to degradation of organic compounds leaching from the epoxy lining (Skjevrak, 1999; Skjevrak, 2000).

Organic compounds leaching from PE bottles and tanks have been the source of taste and odour in water and even a week colour has been experienced because of this migration. Analysis of the water has identified low concentrations of several VOCs, such as ketones (Skjevrak, 1999).

Migration of VOC from water pipes manufactured of HDPE, PVC and PEX has been investigated using static contact with water for three successive test periods each of 72 hours duration according to EN-1420-1 (Skjevrak, 2000; Skjevrak, 2002a and b). The leaching of organic compounds from HDPE pipes showed a considerable variation both in type and amount. Five out of seven tested brands of HDPE pipes showed unacceptable TON values (TON > 3) of test water. Degradation products from phenol-based antioxidants were major migrants from HDPE pipes. VOCs leaching from PEX pipes gave an intense odour of test water. Several of the migrated VOCs were not identified. Oxygenates predominated within the identified VOC with methyl tert-butyl ether (MTBE) as a major component Migration tests of PVC pipes revealed few volatile migrants in low concentrations, and TON assessments did not show significant odour in any of the tests. VOCs leaching from lubricants used for joining of pipes included components such as C6-C11 aliphatic aldehydes, ketones, siloxanes and phenol based anti oxidants. Migration of VOC from HDPE into natural biofilm established in HDPE pipes at turbulent flow conditions is also looked into (Skjevrak, 2002c).

## ABS

### http://www.healthybuilding.net/pvc/pipes_report.html

Acrylonitrile butadiene styrene (ABS) is not chlorinated, but like PVC has highly hazardous manufacturing intermediates, including carcinogens and is difficult to recycle. It is considered only marginally better than PVC environmentally.

### Recycling guide

Acrylonitrile butiadene styrene

http://www.grassrootsinfo.org/index.html?ce/plastics.html

The following recycling code guide is printed with permission from The Green Guide #88 and #89

#1 PETE or PET (polyethylene terephthalate): used for most clear beverage bottles.

#2 HDPE (high density polyethylene): used for "cloudy" milk and water jugs, opaque food bottles.

#3 PVC or V (polyvinyl chloride): used in some cling wraps (especially commercial brands), some "soft" bottles.

#4 LDPE (low density polyethylene): used in food storage bags and some "soft" bottles.

#5 PP (polypropylene): used in rigid containers, including some baby bottles, and some cups and bowls.

#6 PS (polystyrene): used in foam "clam-shell"-type containers, meat and bakery trays, and in its rigid form, clear take-out containers, some plastic cutlery and cups. Polystyrene may leach styrene into food it comes into contact with. A recent study in Environmental Health Perspectives concluded that some styrene compounds leaching from food containers are estrogenic (meaning they can disrupt normal hormonal functioning.) Styrene is also considered a possible human carcinogen by the World Health Organization's International Agency for Research on Cancer (IARC).

#7 Other (usually polycarbonate): used in 5-gallon water bottles, some baby bottles, some metal can linings. Polycarbonate can release its primary building block, bisphenol- A, another suspected hormone disrupter, into liquids and foods. In 1998, the Japanese government ordered manufacturers there to recall and destroy polycarbonate tableware meant for use by children because it contained excessive amounts of bisphenol- A. Other sources of potential bisphenol- A exposure include food can linings and dental sealants.

## #1 pete

http://www.bellaonline.com/articles/art23142.asp

The EPA classifies plastic type #1 PETE as containing a leachable form of DEHA, classified as a "possible human carcinogen"

## Consumer reports bottled water

Source: Consumer Reports, Aug2000, Vol. 65 Issue 8, p17, 5p, 1 chart, 3c.

http://www.angelfire.com/nm/redcollarcrime/tbw.html

Waters bottled in PET plastic generally tasted better than those bottled in HDPE. That was true even within the same brand. Arrowhead Mountain Spring Water, for example, was very good when bottled in PET, which imparted a hint of sweet, fruity plastic flavor (imagine the scent when you blow up a beachball). But Arrowhead was only fair when bottled in HDPE, which made it taste a bit like melted plastic (imagine the smell when you get a plastic container too close to a flame). For waters that come in both kinds of bottle, the Ratings list two scores (and two prices---water is apt to cost more in PET). The only water bottled in PVC plastic, Winn-Dixie's Prestige Premium 100% Spring Water, rated good overall.

BOTTLE BASICS

Bottles can actually affect a water's taste and chemical content. Here are advantages and disadvantages of common bottle materials.

PET (ALSO CALLED PETE)

Short for polyethylene terephthalate, PET is a clear, strong plastic that leaves nothing more than a faint sweet or fruity plastic flavor, if that. Labels for some brands packed in PET play up the "clear" taste of the water inside.

HDPE

High-density polyethylene is the opaque, flexible material of milk containers. It's less expensive than PET but often imparts a slight melted-plastic taste to water. Taste may also be affected by excessive heat or flavors from foods stored nearby.

GLASS

Chemically, glass is inert and imparts no taste whatsoever. But it's heavy and breakable and is seldom used nowadays except for pricey mineral waters and water bottled for bars, restaurants, and hotels.

POLYCARBONATE

Strong and rigid, it's used for compact discs as well as 5-gallon water-cooler jugs. The three water-cooler waters we sampled -Great Bear, Deer Park, and Poland Springs - had no funny flavors. In fact, those waters tasted better than the same products in PET or HDPE bottles. But our analyses showed that polycarbonate sometimes leaves residues of a worrisome chemical, bisphenol-A.

## Consumer confidence report

http://www.rules.utah.gov/publicat/code/r309/r309-225.htm

(30) Benzo(a)pyrene (PAH) (nanograms/l) -Leaching from linings of water storage tanks and distribution lines.

## Building Green on PVC

http://www.buildinggreen.com/features/pvc/pvc.cfm

## Greenpeace PVC ban program

http://archive.greenpeace.org/toxics/html/content/pvc5.html

## Enfvironmental and health effects of PVC

http://archive.greenpeace.org/toxics/reports/cfap/cfapm3.html - 4.0

## The most neglected area of emergency food storage is water

http://www.bagelhole.org/article.php/Water/104/

One of the simplest, but most neglected area of emergency food storage is water. This problem is compounded when home food storage programs rely heavily on dried foods such as beans, wheat and powdered milk. You may have enough calories stored to last six months, but do you have enough water?

One gallon per day per person is the recommended minimum. More realistic though is about two quarts for drinking plus a gallon for washing plus whatever water you might need for cooking. This is the bare minimum.

You don't need to go out and buy specific storage bottles, but not all food household containers are fit for water storage. Plastic gallon milk bottles are safe, but not durable and may start leaking if stored for long periods. Glass gallon bottles like those used for apple cider are also safe, but be careful where you store them. Probably the perfect water storage bottles are the two-liter type soda bottles. If plastic containers are used, care should be taken to assure that they are made of plastic approved for food contact by the Federal Food and Drug Administration. Polyethylene plastic is approved for food contact and is commonly used for containers of various sizes, including 55-gallon drums. Certain types of plastic containers are not intended for food contact (such as vinyl plastic waterbeds, or trash containers) and may leach undesirable chemicals into stored water. Leaching of chemicals from approved plastics is negligible. Water stored in plastic containers should not be stored near gasoline, kerosene, pesticides or similar substances. Vapors from these substances could permeate the plastic and affect the water. Thick-walled polyethylene containers are significantly less permeable to vapors than are thin walled containers, Be certain, when selecting a storage container for water, that it has a tight fitting cap or lid to prevent entrance of contaminants and evaporation of water. Because sunlight has an adverse affect on plastic, water should be stored away from direct exposure to sunlight.

## Shelf Life of Water

The shelf life of water depends on the original quality of the water, the temperature at which it is stored, how much light it is exposed to just to name a few. Many manufacturers of bottled water will include a shelf life on their product.

Treated water out of the tap needs nothing added and should have a shelf life of about 10 years. Untreated water, from a well for instance, should be stored with about 16 drops of chlorine bleach per gallon. Sterilized or disinfected water, stored in clean, food-approved containers with secure lids or caps, should be safe for use even after many years of storage. Replacement of stored water with fresh water should be necessary only if the stored water becomes contaminated in some way or if the container should begin to leak. Be certain to label each container so there will be no question about its contents. Include the date and information on the method of disinfection used.

Stored water may eventually develop a disagreeable appearance, taste, or odor. Under emergency conditions, water that tastes flat can be aerated by pouring the water from one container to another to another about three or four times. Be Careful About Rain Water - Rain water that has been collected should be treated the same as any other unknown water source. Rain water contains small particulates and acid.

## Leaching from Lexan Polycarbonate nalgenes

http://www.sierraclub.org/sierra/200311/lol5.asp

Clear, lightweight, and sturdy polycarbonate plastic bottles are standard equipment for millions of hikers and babies. (They are usually labeled #7 on the bottom; Nalgene is the best-known producer.) Since polycarbonate bottles don’t impart a taste to fluids, many users assume they are safer than bottles made out of other kinds of plastic. But now an accidental discovery has cast doubt on their safety.

Normal wear-and-tear and cleaning of polycarbonate plastic bottles in a dishwasher, Hunt says, could cause the chemical to leach, and the amount of leaching increases as the plastic ages and is degraded by use. A separate study published in July in Environmental Health Perspectives confirmed this finding, and also detected leaching from new polycarbonate plastic.

Theo Colborn, author of the groundbreaking book about endocrine disrupters, Our Stolen Future, calls BPA a "very, very sticky problem. This is a product that’s everywhere, and in everything." (In addition to bottles, BPA turns up in dental sealants and the resin linings of many food and beverage cans.) She recommends washing polycarbonate bottles with mild detergent only, and rinsing well. (Thorough washing is crucial for any reused bottle, because of the danger of bacterial contamination.)

Most at risk, says Colborn, are people with developing endocrine systems: pregnant women and newborns, followed by young children, and women who might get pregnant. Hunt says that if she had an infant, she would switch to polypropylene (#5 PP), which is not known to leach harmful substances. (Other plastics that are not known to leach are #2 HDPE and #4 LDPE. "Single use" plastic bottles made of polyethylene terephthalate [#1 PET or PETE] are not recommended for repeat use because of the risk of bacterial contamination from infrequent and insufficient washing.

Or you could avoid plastic altogether and switch to glass or lightweight stainless steel containers.

—Frances Cerra Whittelsey

November/December 2003

In "Hazards of Hydration," we cited a study about single-use water bottles that appears to have been flawed. While reusing these #1 PET bottles is not a good idea because of risk of bacterial contamination, you probably don't need to worry about them releasing the chemical DEHA. The article has been corrected.

## Safer Plastics for Storing Foods

Green Guide | The Green Guide

by Andreea Matei

http://www.thegreenguide.com/doc.mhtml?i=BGG2&s=saferplastics

Web only | posted February 28, 2003

## Safer Containers: The List

by Andreea Matei

When plastics are the only choice for food storage, look for options with recycling codes #1 PETE, #2 HDPE, #4 LDPE and #5 PP (on the bottom of containers).These are frequently recycled plastics which have not been found to leach toxins into your food.

## On plastic water bottles

By Umbra Fisk

02 Aug 2004

http://www.grist.org/advice/ask/2004/08/02/umbra-bottles/

Let's talk specifics, though, because you point out an apparent conundrum in your question. The contradictions you see in the press are a mix of confusion about types of plastic, misinformation, and bona fide scientific uncertainty about the effects of an entirely new group of substances. Snopes.com addresses purported links between PET (#1) and DEHA (di-2-ethylhexyl-adipate), a potential carcinogen, links which are apparently based on a study later shown to be bogus. PET evidently does not contain DEHA, and the carcinogenic properties of DEHA itself are hotly debated.

Moving on, I would categorically avoid PVC (#3), aka vinyl, for food containers or anything else. It truly is an evil plastic, practically a fount of dioxin. PVC containers and PVC film can contain oft-debated ickies DEHP and DEHA, and some contain softening phthalates linked to liver and kidney damage and testicular problems. Also, polystyrene (#6) is yucky -- it's made of styrene, and you don't want any styrene in your precious bod, trust me.

That leaves us with the winners of this dubious contest: HDPE, LDPE,

## OC&PA: What about cooking with plastics?

http://www.jhsph.edu/Press_Room/articles/Halden_dioxins.html

RH: In general, whenever you heat something you increase the likelihood of pulling chemicals out. Chemicals can be released from plastic packaging materials like the kinds used in some microwave meals. Some drinking straws say on the label “not for hot beverages.” Most people think the warning is because someone might be burned. If you put that straw into a boiling cup of hot coffee, you basically have a hot water extraction going on, where the chemicals in the straw are being extracted into your nice cup of coffee. We use the same process in the lab to extract chemicals from materials we want to analyze.

## PR its cool article

http://www.nalgene-outdoor.com/technical/bpaInfo.html

## EPA’s Endocrine Disruptors Research

For further information on EPA’s Endocrine Disruptors Research Program, please contact the National Program Director for EPA’s Endocrine Disruptors Research Program, Elaine Z. Francis, Ph.D., by telephone at (202) 564-6789, or by e-mail at francis.elaine@epa.gov.

Sent e mail 10/18/04

## Distilled water and methyl chloride

http://www.naturalms.com/newwater.htm

We wouldn't recommend purchasing distilled water from a supermarket that are stored in a plastic container. Many plastics give off toxins such as methyl chloride, a carcinogen which can leach into the water. Glass bottles or stainless steel containers are recommended for storing distilled water. "

## Bisphenol A Is Released from Used Polycarbonate Animal Cages into Water at Room Temperature

http://ehp.niehs.nih.gov/docs/2003/5993/abstract.html

Bisphenol A (BPA) is a monomer with estrogenic activity that is used in the production of food packaging, dental sealants, polycarbonate plastic, and many other products. The monomer has previously been reported to hydrolyze and leach from these products under high heat and alkaline conditions, and the amount of leaching increases as a function of use. We examined whether new and used polycarbonate animal cages passively release bioactive levels of BPA into water at room temperature and neutral pH. Purified water was incubated at room temperature in new polycarbonate and polysulfone cages and used (discolored) polycarbonate cages, as well as control (glass and used polypropylene) containers. The resulting water samples were characterized with gas chromatography/mass spectrometry (GC/MS) and tested for estrogenic activity using an MCF-7 human breast cancer cell proliferation assay. Significant estrogenic activity, identifiable as BPA by GC/MS (up to 310 µg/L), was released from used polycarbonate animal cages. Detectable levels of BPA were released from new polycarbonate cages (up to 0.3 µg/L) as well as new polysulfone cages (1.5 µg/L), whereas no BPA was detected in water incubated in glass and used polypropylene cages. Finally, BPA exposure as a result of being housed in used polycarbonate cages produced a 16% increase in uterine weight in prepubertal female mice relative to females housed in used polypropylene cages, although the difference was not statistically significant. Our findings suggest that laboratory animals maintained in polycarbonate and polysulfone cages are exposed to BPA via leaching, with exposure reaching the highest levels in old cages. Key words: animal caging, bisphenol A, endocrine disruptor, estrogen, leaching, polycarbonate, polysulfone. Environ

## Leaching of mutagens into mineral water from polyethyleneterephthalate bottles.

De Fusco R, Monarca S, Biscardi D, Pasquini R, Fatigoni C.

http://www.ncbi.nlm.nih.gov/entrez/query.fcgi?cmd=Retrieve&db=PubMed&list_uids=2137646&dopt=Abstract

Department of Experimental Pharmacology, University of Naples, Italy.

Polyethyleneterephthalate (PET) was tested as a source of mutagen contamination from bottles used for beverage packaging. PET bottles were filled with mineral water and stored in daylight and in the dark for different periods of time. The water samples were concentrated and the concentrates (non-volatile compounds) tested for mutagenicity with the Ames test (static tests). Total organic carbon (TOC) leaching was determined concurrently. Leaching of mutagens was also studied using dynamic tests; shaking distilled water in PET bottles. New methods were also used to test the leaching potential of both volatile and non-volatile compounds: directly testing the mutagenicity in unconcentrated water stored in PET bottles and growing Salmonella strains directly in the plastic bottles. The results were positive only for the static test, which identified leaching of mutagens after 1 month of storage in PET bottles. This activity was higher after storage in daylight.

## Studies of migration of potentially genotoxic compounds into water stored in pet bottles.

Monarca S, De Fusco R, Biscardi D, De Feo V, Pasquini R, Fatigoni C, Moretti M, Zanardini A.

School of Medicine, University of Brescia, Italy.

http://www.ncbi.nlm.nih.gov/entrez/query.fcgi?cmd=Retrieve&db=pubmed&dopt=Abstract&list_uids=7927074

Coloured polyethylene terephthalate (PET) bottles for carbonated beverages were studied for potential migration of genotoxic compounds. A combined approach, using physicochemical methods and a bacterial short-term mutagenicity test (Ames test) was followed. Standard EEC and US FDA tests for total migration of non-volatile migrant compounds into distilled water were performed, together with modified tests, where freeze-drying instead of evaporation of water was used, in order to measure both volatile and non-volatile chemicals. Gas chromatography-mass spectrometry (GC-MS) analysis was performed on these residues. PET bottles filled with naturally carbonated mineral water were also used for long-term total organic carbon (TOC) and mutagenicity migration studies (up to 6 months' storage). Total migration results for PET bottles were within the EEC and US FDA limits. The use of freeze-drying for the elimination of water enabled much higher total migration data (higher than the limits) to be revealed. Some potentially genotoxic compounds (acetaldehyde, dimethyl terephthalate, terephthalic acid) were identified in these migrant compounds by GC-MS analysis. The tests for TOC migration gave a maximum value after 2 wk storage and the mutagenicity tests on non-volatile migrant compounds gave always negative results

## Aldehyde contamination of mineral water stored in PET bottles.

Darowska A, Borcz A, Nawrocki J.

Department of Water Treatment Technology, Faculty of Chemistry, A. Mickiewicz University, Poznan, Poland.

http://www.ncbi.nlm.nih.gov/entrez/query.fcgi?cmd=Retrieve&db=pubmed&dopt=Abstract&list_uids=14726281Aldehyde contaminations that might accompany production of mineral water stored in PET bottles were investigated. One of the production lines of carbonated mineral water in Poland was monitored and PET bottles commonly used for mineral water storage were evaluated. Formaldehyde and acetaldehyde were the most important carbonyls identified in series of bottled water samples, but also propanal, nonanal and glyoxal were found in water samples from the production line. Aldehydes are present everywhere in the environment and can be determined even in pure water at low microg l(-1) levels. It was observed that the concentration of acetaldehyde in water stored in PET bottles depended mainly on the concentration of acetaldehyde in PET material and could reach more than 200 microg l(-1). The temperature, time of storage and concentration of carbon dioxide gas contribute to the migration of aldehydes from bottle walls to mineral water. Higher pressure of the carbonated waters and not CO(2) itself or lower pH of waters seems responsible for higher concentration of acetaldehyde.

## Evaluation of the migration of mutagens/carcinogens from PET bottles into mineral water by Tradescantia/micronuclei test, Comet assay on leukocytes and GC/MS.

Biscardi D, Monarca S, De Fusco R, Senatore F, Poli P, Buschini A, Rossi C, Zani C.

Department of Life Science, II University of Naples, Naples, Italy.

http://www.ncbi.nlm.nih.gov/entrez/query.fcgi?cmd=Retrieve&db=pubmed&dopt=Abstract&list_uids=12526902

This study monitored the release of mutagenic/carcinogenic compounds into mineral water (natural and carbonated) from polyethylene terephthalate (PET) bottles, using a plant mutagenicity test which reveals micronuclei formation in Tradescantia pollen cells (Trad/MCN test), a DNA damage assay (Comet assay) on human leukocytes and gas chromatography/mass spectrometry (GC/MS) for the characterisation of migrants. The water samples were collected at a bottling plant and stored in PET bottles for a period ranging from 1 to 12 months. Every month some samples were randomly collected and lyophilised, the residual powders were extracted with organic solvents and then analysed by GC/MS and tested for DNA damage in human leukocytes, or reconstituted with distilled water to obtain concentrates for the exposure of Tradescantia inflorescences. Micronuclei increase in pollen was found only in natural mineral water stored for 2 months. DNA-damaging activity was found in many of the natural and carbonated water samples. Spring water was negative in the plant micronuclei test and the Comet assay, whereas distributed spring water showed DNA-damaging effects, suggesting a possible introduction of genotoxins through the distribution pipelines. GC/MS analysis showed the presence in mineral water of di(2-ethylhexyl)phthalate, a nongenotoxic hepatocarcinogenic plasticizer, after 9 months of storage in PET bottles. Copyright 2002 Elsevier Science B.V.

## [Studies on the bottles of mineral water and the foreign plastic like substances]

[Article in Japanese]

Kawamura Y, Sugita T, Watanabe Y, Takano T, Itakura T, Ikegawa T, Yamada T.

http://www.ncbi.nlm.nih.gov/entrez/query.fcgi?cmd=Retrieve&db=pubmed&dopt=Abstract&list_uids=9641831

The containers of mineral water and the foreign plastic substances which were found in the mineral water were investigated. Most of plastic bottles were made of polyethylene terephthalate (PET) and the caps were made of polypropylene (PP), polyethylene (PE) or aluminum. PE liners were attached to some caps. Most of the foreign plastic substances were PET while others were PE, PP, Teflon and rubber. Some bottles had a scratch on the top inside. The origin of most PET fragments was presumed to be scraped off the bottles by the lowering of the injection nozzle during the water filling process. The sources of the other substances were also determined.

## Chemical and in vitro toxicological evaluations of water packaged in polyvinyl chloride and polyethylene terephthalate bottles.

Sauvant MP, Pepin D, Bohatier J.

Faculte de Pharmacie, Laboratoire d'Hydrologie et Hygiene, Clermont-Ferrand, France.

http://www.ncbi.nlm.nih.gov/entrez/query.fcgi?cmd=Retrieve&db=pubmed&dopt=Abstract&list_uids=7589720

This study proposed a new strategy assessing the health risks of mineral water packaging and compared the chemical analytical techniques and some in vitro cytotoxicological assays for the study of PVC and PET materials at the main stages of the manufacturing process of bottles. These evaluations were carried out with food simulant (deionized-endotoxin-tested water) and with natural mineral water in real conditions of packaging and storage (from 0 to 24 months). The complementarity of these two approaches is discussed. Some analytical and cytotoxic abnormalities were detected in the food simulant after contact with the batches of powdered PVC compound, PET resin and their intermediate steps of transformation (PVC-'paraison', PET-'perform'). But these results did not reflect the actual behaviour of the finished PVC and PET bottles, for which no major abnormality was detected in the natural mineral water.

## The bacterial flora of non-carbonated, natural mineral water from the springs to reservoir and glass and plastic bottles.

Bischofberger T, Cha SK, Schmitt R, Konig B, Schmidt-Lorenz W.

Institute of Food Science, Swiss Federal Institute of Technology, Zurich.

http://www.ncbi.nlm.nih.gov/entrez/query.fcgi?cmd=Retrieve&db=pubmed&dopt=Abstract&list_uids=2223521

Quantitative and qualitative determinations of the bacterial flora of non-carbonated natural mineral water at the most important steps during bottling at a large water source yielded the following results: (i) Colony counts (on 1:10 diluted plate count agar, incubated at 20 degrees C for 14 days) for water of the five springs and the mixed water were less than 1 to 4 cfu ml-1. The Gram-negative bacterial flora (n = 50 isolates) showed a very different but constant spring specific species distributions with predominance of either eutrophic fluorescent pseudomonads, oligotrophic non-fluorescent pseudomonads or oligotrophic yellow bacteria. (ii) In the reservoir and immediately after bottling the counts were in the range of 10 cfu ml-1. But nearly 30% of the species of the spring water were no longer detectable and there was a significant increase of Gram-positive bacteria. (iii) After 1 week of storage at 20 degrees C colony counts of more than 10(5) cfu ml-1 were found in plastic bottles, but only about 10(4) cfu ml-1 in glass bottles. Besides, a very distinct change of the composition of the microflora occurred. In glass bottles slow-growing oligotrophic non-fluorescent pseudomonads, yellow bacteria and Acinetobacter predominated. In plastic bottles fast-growing eutrophic and mesotrophic fluorescent pseudomonads, Flexibacter and Acinetobacter were dominating. In mineral water, bottled into thoroughly cleaned glass bottles, colony counts of more than 10(5) cfu ml-1 were found within 4 days. In bottles, cleaned mechanically as usual, the increase was significantly slower with a maximum of only 5 x 10(3) cfu ml-1 after 8 days. The results of inoculation experiments in sterile filtered mineral and distilled water led to the suggestion that the difference between the two types of bottles is caused firstly by an inhibition of growth due to residues of cleaning detergents in the glass bottles. Growth promotion by dissolved organic substances in the plastic bottles only played a minor role. After repairing of the pump at a depth of 300 m in a warm mineral water spring, the colony counts at 20, 37 and 42 degrees C on 1:10 diluted and normal plate count agar increased beyond the limits required by the EC directive for mineral water stored a month. Then colony counts decreased slowly and reached the initial level after 1 year, except for the colony counts 1:10 diluted agar at 20 degrees C which stabilized at a relatively high number and a significant alteration of the microflora.(ABSTRACT TRUNCATED AT 400 WORDS)

## Don’t worry about it-Plastics Council

http://www.newton.dep.anl.gov/askasci/chem00/chem00959.htm

All the plastics coded 1 through 7 can be made in grades that are approved

for use as food containers.  You do not really need to worry about the

leaching of chemicals from the plastics.  Even the plastics that can exude

some components upon prolonged content do so in such low amounts that it is

not a health issue.  The chance of being injured by a car as you are on your

way to the store to buy bottled water is much, much greater than the chance

that your health will be impaired by drinking water from a plastic

container.

Richard E. Barrans Jr., Ph.D.

PG Research Foundation, Darien, Illinoi

# Leaching from fiberglass

## Leaching of organic contaminants from GRP pipe

http://www.fwr.org/waterq/dwi0032.htm

A wide range of contaminants were found to leach into drinking water  from GRP pipe including a range of phthalates and styrene. The leaching rates were appreciable although depletion with time would be expected.

## Leaching off substances from products used in contact with water intended for human consumption

www.dwi.gov.uk/cpp/pdf/protocol1.pdf

| Thermoplastic materials |  |  |  |
| --- | --- | --- | --- |